## Slide 1
10-December -2020
MUSASHI AUTO PARTS INDIA PVT. LTD.
K0PA MISSION NOISE

## Slide 2
K0PA-Mission Noise
Date ： 2020/Dec/10
Reported ： Musashi Auto Parts India Pvt. Ltd
Approval
Check
Issued
Subject ：- NOISE REPORTED AT HMSI
Anoop
Satoshi/Prashanth
Umasankar
■Contents of report |  |  | 
 | Contents | Page | Cum Time Sec
1 | Problem and Primary Causes | 3 | 10
2 | Case 1.Teeth Damage | 4~7 | 80
3 | Case 2.OBD, Lead and Profile | 8 | 10
4 | Lead and Profile Study and Optimization | 9~11 | 60
5 | OBD Study and Optimization | 12~13 | 40
6 | Recent N2 Noise parts report | 14 | 20
 | Total |  | 220 Sec
Primary Focus
Gear Counter
Shaft Drive
Model: K0PA
Gear Comp Final
a.Gear Final
b.Shaft Final
Gear Comp Counter
a.Gear Counter
b.Shaft Counter
Shaft Drive

## Slide 3
PROBLEM AND PRIMARY CAUSES
Mission Noise
TTCE OK
TTCE NG
a.LEAD AND PROFILE
b.OBD
TEETH DAMAGE
SD
GC
To be Studied for Improvement
Reported From Customer
OK
Case1
Case 2
Gear Counter Teeth Damage is First Focus
TTCE(Tooth-To-Tooth Composite Error): Measured error between adjacent teeth of the part gear using a master gear.
Nicks or Damages in the teeth will show up as tooth-to-tooth error

## Slide 4
CASE 1-TEETH DAMAGE
PROCESS FLOW
TURNING2
TURNING1
MATERIAL RECIEVING
BROCHING
SHAVING
GRT
ASSY. SC & GC
HT
SHOT BLASTING.
JIG LOADING
HOBING
DISPATCH TO HMSI
Outflow
Occurrence
Occurrence
Teeth Damage Occurrence and Outflow area Identified

## Slide 5
TEETH DAMAGE-DAMAGE COMPARISON
Lower TTCE Damages to be Analysed
Customer Reported Dents:-
Dent Location
Tip Area
Semitopping
Bottom Edge
Inhouse Reported Dents:-
SLNO | TTCE (0.016 Max) | Hard/Soft
1 | 0.024 | Hard
2 | 0.035 | Hard
3 | 0.026 | Hard
4 | 0.028 | Hard
5 | 0.030 | Hard
TTCE
Dent Location
Tip Area
Teeth OD
Semitopping
SLNO | TTCE (0.016 Max) | Hard/Soft
1 | 0.045 | Soft
2 | 0.072 | Soft
3 | 0.050 | Hard
4 | 0.046 | Hard
5 | 0.081 | Soft
Higher TTCE part not Flowing to Customer
Soft Dents Majorly detected at Inhouse

## Slide 6
Root Cause | Action | Before | After | Resp | Status
Part Touching at Unloading Pallet of Shaving due to pallet worn out and Broken | Output Pallet Design Changed to avoid breakages and Part to part Hit. (L1, L2 Implemented) |  |  | Hubli/Gaurav | Ο
Parts Slipping from Slots in Bin and Possible to Touch Each other when Transport | Immediate: NG Bins Identified and Removed From System Permanent: 100% Inspection of Bin Before Issue to Line |  |  | Krishna | Ο
OBSERVATIONS
Conclusion:
TTCE OK parts also Create Noise.
Small Nicks at tip Not Detected at MAP ID.
Nature of Damage: Damage on OD which bulged to Flank
TTCE OK Observed on Some Noise parts even though Small Nick Visible
Part 2
Part 1
Touching Corners/OD When unloaded part Tilts
Part 3
Part 4
Pallet
Part 1
Part 2
Part 3
Part 4
Firm holding of Parts with new Designed Pallet
TEETH DAMAGE-OBSERVATIONS AND ACTION
ACTIONS
Occurrence Action Completed
Chart: TTCE Comparison
| 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
With MG | 0.012 | 0.01 | 0.009 | 0.008 | 0.013 | 0.01 | 0.011 | 0.008 | 0.01 | 0.011
Wth SD | 0.022 | 0.019 | 0.018 | 0.018 | 0.024 | 0.02 | 0.022 | 0.021 | 0.022 | 0.018
Limit | 0.016 | 0.016

## Slide 7
 | Root Cause | Action | Resp | Status
Outflow | 1.Existing Master gear Design not able to detect Small Nicks | Immediate: Additional Roll Testing added with Mating Part established on Temporary basis. Permanent: 1.Master Gear Design Improvement to be Done (First round of Discussion with maker over) | Giridhar Narendra | Ο Feb-21
 | Small nicks Observed on the parts which is showing TTCE OK in GRT | Sense/Feeling Based Detection Started and Suspected parts Reworked through Burnishing process and Re-Verified through GRT | Giridhar | Ο
1
2
Small Nick at Tip escapes from Master Gear
Small Nick also create noise effect due to Contact Pattern
1
2
Suspect:
Detection Mechanism
Verification:
Vehicle Condition Simulation with SD
Phenomenon:
Master gear Design cannot Replicate Mating Part Condition
Conclusion:
Master Gear Design Improvement to be done
Observation at Noise Parts:
TTCE Below 0.007 also create Noise at Vehicle (0.016 max)
Burnishing Process
Burnishing will take out all fine Dents on teeth Tip.
GRT With Mating Part
OBSERVATIONS
ACTIONS
TEETH DAMAGE-OBSERVATIONS AND ACTION
Outflow Weakness Identified and Addressed
GRT With Master Gear

## Slide 8
EFFECTIVENESS
Weakness Analysis Started
Chart: Mission Noise Cases Reported From HMSI
| 44116 | 44117 | 44118 | 44119 | 44120 | 44121 | 44122 | 44123 | 44124 | 44125 | 44126 | 44127 | 44128 | 44129 | 44130 | 44131 | 44132 | 44133 | 44134 | 44135 | 44136 | 44137 | 44138 | 44139 | 44140 | 44141 | 44142 | 44143 | 44144 | 44145 | 44146 | 44147 | 44148 | 44149 | 44150 | 44151 | 44152 | 44153 | 44154 | 44155 | 44156 | 44157 | 44158 | 44159 | 44160 | 44161 | 44162 | 44163 | 44164 | 44165 | 44166 | 44167 | 44168 | 44169 | 44170 | 44171 | 44172 | 44173 | 44174 | 44175
Cases Reported | 21 | 10 | 20 | 1 | 1 | 5 | 1
GRT with SD
Issue Reported even after Actions
Re- Analysis and Actions

## Slide 9
 | 4M | Weak Area | Root Cause | Action | Status
 | Man | Detection Level By Operator not enough | Skill Level not sufficient as New method of inspection | Limit Sample Introduced Training Conducted with Limit Sample Ishiwara Test Conducted Dedicated Manpower Decided for Inspection | 
 | Machine | Different Reading between Two GRT | Top Center Play observed at One GRT (Play:0.025) | Top Center play arrested (0.006) | 
 | Material | - | - | - | -
 | Method | Awareness Level not enough among the Inspectors | Existing Standardization weak as New Method Of Inspection | Inspection Startup Check Sheet Provided Mating Height level Standardized | 
Weak Point Identification-Outflow
GAP ANALYSIS
Focus: GRT with Mating Part

## Slide 10
GAP ANALYSIS
Effectiveness Monitoring Continuously.
EVIDENCES
Before: 2 mm
After: 6 mm

Chart: GRT Reading Comparison-Before Correction
GRT 1 | 0.006 | 0.035 | 0.012 | 0.017 | 0.013
GRT 2 | 0.007 | 0.035 | 0.016 | 0.026 | 0.016
Target | 0.016 | 0.016 | 0.016 | 0.016 | 0.016
Chart: GRT Reading Comparison-After Correction
GRT 2 | 0.007 | 0.035 | 0.016 | 0.026 | 0.016
Target | 0.016 | 0.016 | 0.016 | 0.016 | 0.016
GRT 1 | 0.006 | 0.035 | 0.013 | 0.025 | 0.016
Play at This Center

GRT 1 identified as Problematic and Corrected
Measuring Hight Standardized to replicate the Situation at Customer.
SUMMARY ISHIWARA |  |  |  |  | 
SL | Name | Defective Samples Verified | Correct Judgement | In Correct Judgement | Pass/Fail
1 | Vandana | 6 | 6 | 0 | P
2 | Pushpalatha | 6 | 6 | 0 | P
3 | Naveen | 6 | 6 | 0 | P
4 | Maruti | 6 | 6 | 0 | P
5 | Guruprasanna | 6 | 6 | 0 | P
6 | Prabhu | 6 | 6 | 0 | P
7 | Harish | 6 | 6 | 0 | P
8 | Mithun | 6 | 6 | 0 | P
9 | Ramesh DG | 6 | 6 | 0 | P
10 | Varalakshmi | 6 | 6 | 0 | P
11 | Madhusudhanan | 6 | 6 | 0 | P
12 | Sachin | 6 | 6 | 0 | P
13 | Naveen(767) | 6 | 6 | 0 | P
14 | Arun | 6 | 6 | 0 | P

Inspectors List
Ishiwara Result
Center Play Correction
Initial Start-Up Check Sheet

## Slide 11
GAP ANALYSIS
Effectiveness Monitoring Continuously.
Weak Area Identification-OCCURRENCE
 | 4M | Weak Area | Root Cause | Action | Status
 | Man | Handling practice | Handling awareness among the people reduced as new manpower added to System | Thorough Training Given to Operators with reference to Customer Detected parts and Internal Detected Parts | 
 | Machine | Gear Line: Part to Part Touching at Unloading. (Line 1 and 2) | Gantry Unloading part touches to parts available in unloaded pallet due to Pallet Hight More | Pallet Hight Reduced | 
 |  | Gear Line: Line 2, Part Drop inside machine | Part Dropping from Part Carrying Pocket at Shaving Unloading Area | Wear out part Replaced Life monitoring started for Replaced part to avoid failure in Future | 
 | Material | - | - | - | 
 | Method | After Shot Blasting: Frequent Trolly Fall down | Trolly wheels Small In Size which Leads to falling | Trolly wheels replaced by Bigger Wheels Dedicated trolly provided for Gear Counter with Identification | 

## Slide 12
GAP ANALYSIS
Effectiveness Monitoring Continuously.
EVIDENCES



Before
After
Identification for Gear Counter Dedicated Trolly
Before
After
Marking made to Avoid overloading
Before
After
Worn out Unloading Pocket Replaced
Training at Gemba

## Slide 13
EFFECTIVENESS
Effectiveness Monitoring Continuously.
Chart: Mission Noise Cases Reported From HMSI
| 44116 | 44117 | 44118 | 44119 | 44120 | 44121 | 44122 | 44123 | 44124 | 44125 | 44126 | 44127 | 44128 | 44129 | 44130 | 44131 | 44132 | 44133 | 44134 | 44135 | 44136 | 44137 | 44138 | 44139 | 44140 | 44141 | 44142 | 44143 | 44144 | 44145 | 44146 | 44147 | 44148 | 44149 | 44150 | 44151 | 44152 | 44153 | 44154 | 44155 | 44156 | 44157 | 44158 | 44159 | 44160 | 44161 | 44162 | 44163 | 44164 | 44165 | 44166 | 44167 | 44168 | 44169 | 44170 | 44171 | 44172 | 44173 | 44174 | 44175
Cases Reported | 21 | 10 | 20 | 1 | 1 | 5 | 1 | 5 | 4 | 4 | 10 | 4 | 7
GRT with SD
Continuously Monitoring the Effectiveness, Internal and External
Actions Completions
Zero Dent Noise issues from 25th Nov
Re- Analysis and Actions

## Slide 14
Lead and Profile and OBD to be Focused
Gear Counter
Shaft Drive
Ο
Ο
Ο
Ο
CASE 2-OBD AND LEAD AND PROFILE STUDY
Noise Parts Dimensional Report
Nature wise and Spec wise NO ISSUE OBSERVED
Scope for improvement to be identified from MP monitoring
Lead and Profile- Gear Counter and Shaft Drive
OBD –Gear Counter and Shaft Drive
STUDY ON NOISE PARTS
Result
FOCUS AREAS FOR NOISE IMPROVEMENT

## Slide 15
Gear Counter Lead Crowning to be Improved
Lead and Profile Current Situation (Shaft Drive-Regular MP Parts)
Ο
Ο
Ο
Ο
Ο
All OK
CASE 2- LEAD AND PROFILE STUDY
Parameter | Spec | Min |  | Max | 
 |  | L | R | L | R
FA | 0~10 | 8.4 | 5.6 | 9.5 | 8.6
TC | 0~4 | 0.9 | 0.4 | 2.6 | 2.2
FH | -10~10 | -3.4 | 1.9 | -2.3 | 6.3
CRN | 0~6 | 2.5 | 2.6 | 3.6 | 3.2
Lead and Profile Current Situation (Gear Counter-Regular MP Parts)
Ο
Ο
Ο
Ο
Parameter | Spec | Min |  | Max | 
 |  | L | R | L | R
FA | 0~10 | 4.5 | 2.5 | 7.4 | 4.3
TC | 0~4 | 1.4 | 1.5 | 3.3 | 2.6
FH | -6~6 | -0.4 | -1.9 | 3.3 | 1.9
CRN | 0~6 | 1.1 | 1.2 | 2.3 | 2.7
Lead crowning Improvement scope to be Studied

## Slide 16
Gear Counter
Shaft Drive
Area of Contact
Area of Contact
Low CRN
High CRN
Gear Counter Lead Crowning level Optimized
Lead Crowning Target Optimization to be Considered
Shaft Drive
Gear Counter
CONTACT PATTERN CHECK
Parameter | Improvement Point | Improvement Action | Target | Resp | Status
Lead Crowning (CRN) | Gear Counter Crowning Target to be Optimized | 9 Point studies to be taken and Soft and Hard Target to be Finalized | 20.10.2020 | Hubli/Harish/Anoop | Ο
CASE 2- LEAD AND PROFILE STUDY

## Slide 17
LEAD CROWNING FOR ALL LINE IMPROVED
CASE 2- LEAD AND PROFILE STUDY
RESULT
Chart: CRN TRAIL 1 & 2 TREND
| 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
 | 2.5 | 3.1 | 2.8 | 2.6 | 2.4 | 2.2 | 2.4 | 2.6 | 2.3
HARD | 2.6 | 2.3 | 2.3 | 2.7 | 2.3 | 2.4 | 2.5 | 1.8 | 2.8
HARD | 3.8 | 4 | 3.6 | 3.7 | 3.7 | 3.3 | 3.2 | 4.4 | 3.2
trail-2 | 3.5 | 3.9 | 3.9 | 3.6 | 3.6 | 4 | 3.3 | 3 | 3.9
SPEC MAX | 6 | 6
SPEC MIN | 0 | 0
Chart: CRN-Before
| 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
Ff L Bfe
Ff L Aft | 1.8 | 2.1 | 1.4 | 1.6 | 1.7 | 1.8 | 1.8 | 1.7 | 1.8 | 1.7 | 1.8 | 1.7 | 1.8 | 1.3 | 1.1 | 1.8 | 1.3 | 1.7 | 1.9 | 1.4 | 1.7 | 1.3 | 2.3
Ff R Bfe
Ff R Aft | 1.9 | 1.2 | 2 | 1.8 | 1.8 | 1.8 | 1.7 | 1.8 | 1.8 | 1.8 | 1.8 | 1.8 | 1.7 | 1.6 | 1.6 | 1.6 | 1.9 | 1.4 | 1.6 | 1.9 | 1.8 | 1.8 | 2.7
 | 6 | 6
min | 0 | 0
LH
RH
Before
After
Chart: CRN TREND LINE WISE-AFTER ALL TRIALS
| 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
 | 3.5 | 3.7 | 3.2 | 3.4 | 3.7 | 3.6 | 3.8 | 3.9 | 3.7
HARD | 3.8 | 3.3 | 3.5 | 3.7 | 3.8 | 3.3 | 3.7 | 3.8 | 3.5
HARD | 3.8 | 4 | 3.6 | 3.7 | 3.7 | 3.3 | 3.2 | 4.4 | 3.2
trail-2 | 3.5 | 3.9 | 3.9 | 3.6 | 3.6 | 4 | 3.3 | 3 | 3.9
SPEC MAX | 6 | 6
SPEC MIN | 0 | 0
HARD | 3.9 | 4 | 3.7 | 3.5 | 3.8 | 3.3 | 3.7 | 3.8 | 3.8
HARD | 3.8 | 3.9 | 3.6 | 3.7 | 3.8 | 3.9 | 3.7 | 3.8 | 4
LH
RH
LH
RH
LH
RH

## Slide 18
OBD Soft Spec Optimized to bring final OBD to Mean Level.
OBD-Comparison
Gear Counter
∆
Ο
∆
OK
Improvement Required
∆
Shaft Drive
CASE 2- OBD
Parameter | Scope for Improvement | Action | Target | Resp | Status
OBD | Gear Counter OBD Maintained Mean to USL | Soft Spec Optimized to Achieve Mean Level. (At all lines Implemented) | 30.10.2020 | Narendra/Anoop/Hubli | Ο

## Slide 19
CASE 2- OBD
RESULT
Chart: GC OBD Trend
| 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2
SOFT | 68.966 | 68.965 | 68.966 | 68.967 | 68.966 | 68.968 | 68.964 | 68.962 | 68.964 | 68.962 | 68.967 | 68.97 | 68.966 | 68.964 | 68.966 | 68.962 | 68.964 | 68.96 | 68.962 | 68.966
HARD | 68.989 | 68.984 | 68.992 | 68.994 | 68.985 | 68.99 | 68.998 | 68.992 | 68.996 | 68.986 | 68.982 | 68.984 | 68.992 | 68.996 | 68.986 | 68.992 | 68.996 | 68.992 | 68.99 | 68.987
Soft | 68.975 | 68.945
Hard Spec | 69.013 | 68.947
Soft Spec
Soft Actual
Final Spec
Final Actual
Before
After
Chart: Final OBD Level- All Lines
| 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
Line 1 | 68.984 | 68.983 | 68.989 | 68.985 | 68.989 | 68.989 | 68.988 | 68.99 | 68.991 | 68.994 | 68.993 | 68.992 | 68.989 | 68.99 | 68.992 | 68.987 | 68.99 | 68.994 | 68.99 | 68.992 | 68.991 | 68.99 | 68.991 | 68.984 | 68.982 | 68.99 | 68.991 | 68.985 | 68.986 | 68.981
Line 2 | 68.985 | 68.98 | 68.981 | 68.985 | 68.981 | 68.984 | 68.982 | 68.982 | 68.985 | 68.982 | 68.985 | 68.984 | 68.984 | 68.98 | 68.982 | 68.98 | 68.988 | 68.988 | 68.982 | 68.981 | 68.982 | 68.991 | 68.982 | 68.98 | 68.982 | 68.983 | 68.991 | 68.99 | 68.981 | 68.982
Line 3 | 68.988 | 68.989 | 68.987 | 68.987 | 68.988 | 68.982 | 68.989 | 68.988 | 68.989 | 68.991 | 68.992 | 68.993 | 68.992 | 68.992 | 68.994 | 68.993 | 68.982 | 68.99 | 68.981 | 68.981 | 68.981 | 68.984 | 68.982 | 68.983 | 68.982 | 68.982 | 68.992 | 68.991 | 68.982 | 68.981
USL | 69.013 | 69.013
LSL | 68.947 | 68.947

## Slide 20
EFFECTIVENESS

## Slide 21
THANK YOU!