## Slide 1
17th-Feb -2021
MUSASHI AUTO PARTS INDIA PVT. LTD.
GEAR COMP FINAL THREAD MISS
Model:K0PA

## Slide 2
1. Overview | Parts Name :GEAR COMP, FINAL Model: K0PA
1-2. Number of Claims | 01 Vehicle
1-3.Occurance Lot No. | MAP Invoice No: 3196
1-4. Cause of Occurrence | Thread Operation Not available
1-4. Countermeasure Details | <Immediate Action ＞ 100% Parts checked Identify Process Verify-Occurrence and Outflow
1-5. Affected Range | 2412 Nos (Invoice No :3196)
OVERVIEW
Segregation Details:
SLNO | LOCATION | Total QTY | Checked QTY | NG QTY
1 | HMSI-3F | 8300 | 8300 | 0
2 | FG | 4320 | 4320 | 0
3 | HT | 3700 | 3700 | 0
4 | Soft | 2050 | 2050 | 0
 | Total | 18370 | 18370 | 0
Part: Gear Comp, Final
Model: K0PA
Report Date:30.01.2021
Thread
OK
Thread Miss

## Slide 3
TRACEABILITY
Summary:
The Suspected Lot Produced in soft at 22.01.2021.
There is no Change Point Available on Particular Date.
Analysis to be done according to the Observations at Claim Part

## Slide 4
OBSERVATION
HEAT TREATMENT
JIG SETTING
THREAD ROLLING
TURNING 2
ROLL TESTING
EDDY CURRENT TESTING
MATERIAL STORAGE
COLD FORGING
STRAIGHTENING
TURNING 1
LASER MARKING
RUNOUT INSPECTION
THREAD ANNEALING
SHOT BLASTING
AXIS GRINDING
ASSY WITH GEAR
Occurrence
OIL APPLICATION AND DISPATCH
Outflow
DEFECT MAPPING BY PROCESS SEQUENCE
PHYSICAL OBSERVATIONS AT PART
Parameter | Spec | Actual | Judgement | Remarks
Pre Roll Dia | 14.890~14.910 | 14.906 | OK | Thread Not Missed Due to Pre-Roll Dia Undersize
Other Observations:
SL No | OBSERVATION | INDICATION | RESULT
 | Yellow Mark at Shaft Face | Eddy Current Test Over | DEFECT SKIPPED
 | ’M’ Alphabet available on Gear Face | GRT Over, Associate Indication | GRT OK PART
 | No feed mark near Grinding Undercut | Line Identification | Line 1
2
1
Occurred at Thread Rolling
Outflow Miss Happened from Eddy Current Testing
3
1
2
3
CLAIM PART IMAGES

## Slide 5
Burr from Turning 2, Which Swirl on the Stopper and Later can transfer to Rollers
ANALYSIS-OCCURRENCE
Thread Miss Happens, when Manually Stops and Restarts Line for Burr Clearing
FACTOR ANALYSIS
Sl No | POSSIBLE CAUSES | VERIFICATION | RESULT
1 | Dropped part miss handling | There is no dropped part recorded, there is no damage on the defect shaft | O
2 | Machine power cut | No power cut on that day | O
3 | Thread rolling part present sensor fault | Part present sensor working - incase of not working gantry don't run | O
4 | Thread head center sensor fault | Head center sensor working - incase of not working gantry don't run | O
5 | Mistake in Line Operation when Burr clearing from Thread Rolling Machine | Stops the line Manually to Remove the Burr and Thread miss Happens when restart the Line | X
6 | 1/50 measuring frequency not followed | 1/50 inspection followed as per frequency | O
7 | Alarm handling time Improper handling | No alarm generated on that day <In change point record> | O
8 | New manpower run the line | Manpower got skill according to Process requirement | O
Rollers
Part
Burr
Due to Improper location of Part on Rollers Cycle will not be Started
What Happens If Burr present between part and Rollers?

## Slide 6
1
2
Turning 2
Gantry
Thread Rolling
O/P Jig
Cycle Start
Gantry Start
Man Intervention
Turning 1
I/P
OK
Ο
Ο
ANALYSIS- OCCURRENCE MECHANISM
Man Intervention for Manual Operation of Parts in case of Burr Removal
Gantry
Auto Operation From Input to Output
Manual Operation
Part Removal
Burr Cleaning Part Re Placing at Locator
Cycle Start
Gantry Start
Manual Break In Operation after Turning 2 for Burr Removal

## Slide 7
ANALYSIS- OCCURRENCE MECHANISM
Logic Change to be Considered to avoid failures in Future
Step | Why1 | Why2 | Why3 | Why4 | Why5
Occurrence | Thread operation miss happened after manual stop of Auto line | Gantry picked the part from Thread Rolling with out Threading Operation | After line reset, gantry started and picked without thread part | Gantry Picks the part even Thread Rolling ‘Cycle Start’ Not activated | Existing logic Allows The Gantry to Pick the part Before Thread Rolling ‘Cycle Start’
Abnormal

1
Manual Operation
Part Removal
Burr Cleaning
Part Re Placing at Locator
Cycle Start
Gantry Start
Manual Break In Operation after Turning 2 for Burr Removal
Mistake done when Re-Started the Line

## Slide 8
ACTIONS- OCCURRENCE
BEFORE
AFTER
Existing Logic: Gantry will Pick the Part from Thread rolling without Thread Roll ‘Cycle start’ also
Manual Part Handling SOP
OJT
Changed Logic: Gantry will Pick the Part from Thread only when Thread Roll ‘Cycle Start’ is Hit
1.OCCURRENCE ROOT CAUSE |  | 1.OCCURRENCE COUNTERMEASURE |  | TARGET DATE | RESP. | STATUS
2B | Existing logic Allows The Gantry to Pick the part Before Thread Rolling ‘Cycle Start’ when Manual Stop and Restart | 2B | Gantry movement to be interlocked with thread rolling ‘Cycle start’ at manual restart also-(interlock logic: if cycle start not hit, gantry will not Pick the part from Thread Rolling) | 03/02/2021 | SURESH & NIJO | O
Why Manual Stop Due to Long Burr ?

## Slide 9
ACTIONS- HOW TO ELIMINATE BURR
Long Burr Avoided by Burr Breaking
Step | Why1 | Why2 | Why3 | Why4 | Why5
Occurrence | Line Manual stopped to correct the Abnormal Situation | Burr Present on the Thread Rolling Machine from Turning 2 | At Turning 2 Some Burr Swirls on the part and comes till Thread Rolling | Long Burrs available after Turning2 | Breaking of burr not happened
Burr
1.OCCURRENCE ROOT CAUSE |  | 1.OCCURRENCE COUNTERMEASURE |  | TARGET DATE | RESP. | STATUS
1A | In Roughing Cut Burr Generated | 1A | Dwell Time of 0.1 Sec Added in Roughing Cut | 03.02.2021 | Praveen, prabhu | O
Breaking of Burr at Turning 2
Parameters
Spec: 0.4~0.5
0.2
As Per Spec
As per Spec
No Long Burr
Long Burr Present
Input Stock
Cutting Method
Tool
Finishing
Roughing
Tool Path
Judgement
Ο
∆
Actual
Sub Factors
Factors
Target
Ο
Ο
Ο

## Slide 10
ACTIONS- EVIDENCE
BEFORE
AFTER
No Mention of Dwell Time in Before tool Path
Dwell time Added in Tool Path
Standardization done

## Slide 11
Red Bin
Yellow Bin
Blue Bin
ANALYSIS-OUTFLOW
NG CONDITION
Part Kept on Tester
Previous Test OK Part Kept at Table
Test and Result
Marking on Previous Test NG Part also Marked OK
Error Reset
Zero Setting
1
2
1
2
Cause:
Associate’s Confusion lead to Skip of NG Part
Test Result
Part @ Test
Part after Test
Input
Output
3
EDDY CURRENT TESTING
POSSIBLE CAUSES | VERIFICATION | RESULT
Not detecting at eddy current | NG Part verified in Eddy Current Testing and found detecting | O
No buzzer or lamp after ng detection | Buzzer and lamp working properly | O
Ng detected part not treated as per ng handling procedure | NG part skip suspected as yellow mark available on the part | X
Man Skill to Identify NG Detection | ISHUWARA test Found OK | O

## Slide 12
ACTION-OUTFLOW
Method Strengthening Done to Avoid Inspection Skip
BEFORE
RYB Bins kept at Right Side of Operator (O/P Side)
RYB Bins Relocated to Left Side, Red Bin Kept near Hand
Associate’s Confusion lead to Skip of NG Part
RYB Bins at Right Hand Side
RYB Bins Shifted To Left Side
Primary Cause
Root Cause
Action
Status
Ο
Ο
AFTER
Improper Habit of Keeping Parts at Table After Test
Training given to Operator and SOP Updated
Eddy Current Flow Standardization
Counter Verification for NG part Detected V/s Actual
Ο
Ο
Input Part Pick
Keep at Table
Remove already Tested part
Keep at Table
Load Input For Testing
Mark Early Tested Part
Keep In Bin
Part Pick
Remove already Test part
Load Input For Testing
Mark Early Tested Part
Keep In Bin
BEFORE
AFTER
1
2
3
4
1
3

## Slide 13
Counter V/s Physical parts Verification
ACTION-OUTFLOW
4
3
BEFORE
AFTER

## Slide 14
POKA YOKE TO PREVENT OUT FLOW TO EDDY CURRENT TESSTING
Thread Missing Detection Will be happening at Pressing So No Outflow up to Eddy Current Testing
Type of Control :Poka Yoke
Process :Gear Pressing
Purpose: To Avoid Thread Miss Part outflow up to Eddy Current Testing
BEFORE
AFTER
Without Thread Part
Not Sensing
With Thread Part
Sensing
POKA YOKE WORKING
Only Spline Inspection
Thread Miss Poka Yoke Added
1
2
1
2
Without Thread get inserted to Bush and No Sensing,
No Signal to Pressing
Thread Pushes the bush and get sensed,
Give signal to Pressing
Shaft
Spline Gauge
Thread Detection Unit
Pressing Process
Gear
Moving Down
Will not Move

## Slide 15
Chart: Thread Miss Report at HMSI
| 44226 | 44227 | 44228 | 44229 | 44230 | 44231 | 44232 | 44233 | 44234 | 44235 | 44236 | 44237 | 44238 | 44239 | 44240 | 44241 | 44242 | 44243
Thread Miss at Customer | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
FOLLOW UP
STANDARDIZATION
EFFECTIVENESS
Zero Report Till Date
Claim Part
Action
Effectiveness found OK after Actions
Chart: Thread Miss Report at Internal
| 44230 | 44231 | 44232 | 44233 | 44234 | 44235 | 44236 | 44237 | 44238 | 44239 | 44240 | 44241 | 44242 | 44243
Thread Miss at Customer | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Action
Zero Report Till Date
Same Action Implemented at Line 2 Also

## Slide 16
Thank You